## Slide 1
Effect of neutron irradiation in the VVER-1000 reactor on the characteristics of secondary phases in zirconium alloys E110 and E635
© A.V.Obukhov, G.P.Kobylyansky, S.S.Sagalov, and A.R.Belozerova, 2019 (JSC “SSC RIAR”, Dimitrovgrad)
XI Reactor Material Science Conference, Dimitrovgrad,
Russia, 27-31 May 2019

## Slide 2: Introduction
Secondary phase precipitates in zirconium-based alloys which have been used as materials for the VVER-1000 core components, are structural constituents and they go through different changes under irradiation.
Changes in the characteristics of secondary phases can lead to changes in the operational performance of the nuclear reactor core components, for instance, fuel claddings and guide tubes, with a potential impact on their operational integrity. Therefore, it is considered of great importance to study changes in phase composition of zirconium alloys E110 and E635 to verify operational integrity of components made of the aforesaid alloys during the entire operational lifetime.
This paper is focused on investigation of the E110 (Zr-1%Nb) phase composition as it is a fuel cladding materials and E635 (Zr-1%Nb-0.4%Fe-1.2%Sn) phase composition as it is a guide tube materials after their operation in the VVER-1000 reactor. In particular, described here are changes in the elemental composition of β-Nb and Laves phases.
2

## Slide 3: Equipment used
Transmission electron microscope enabling operation at an accelerating voltage of 200 kV
Electron probe X-ray microanalysis instrument which employs the INCA X-MAX TEM 80 system
Electrolytic equipment TENUPOL-5 designed for electrolytic thinning
Semiconductor detector ORTEC GEM10P4-70PL made of high purity germanium and multichannel analyzer ORTEC DSPEC jr 2.0 for gamma-spectrometry
Equipment for sample preparation in the hot cell
3

## Slide 4: Objects under investigation
4
Operating time, yr. | Object under investigation | Alloy | Damage dose, dpa | Irradiation temperature, оС
3 | Fuel cladding | E110 | 2 - 11 | 300-340
 | Guide tube | E635 | 2.5 - 10 | 290-320
5 | Fuel cladding | E110 | 2 - 17 | 300-340
 | Guide tube | E635 | 2.5 - 16 | 290-320
The specimens were cut out from several irradiated fuel claddings and guide tubes at different elevation levels. Their operating time was different too. Thus, it was possible to obtain irradiation-induced damage data as to different extent of damage and irradiation temperatures.

## Slide 5: Irradiation temperature
The irradiation temperature of the test specimens was obtained based on the calculated temperature data profile on the surface of fuel cladding (black points) and guide tube (red points) throughout the height [1].
5
[1] - V. V. Svetukhin. Modeling of corrosion kinetics for Zr claddings of the VVER-1000 fuel rods/ V.V. Svetukhin, A. E. Novoselov, G. P. Kobylyansky[etc]// Collected papers. Modeling of reactor materials performance under irradiation. – under the editorship of V. V. Svetukhin, Ph.D, V. N. Golovanov, Ph.D and V. D. Risovany – Ulyanovsk: Ulyanovsk state University. – 2007. - Pp.91-98

## Slide 6: Damage dose estimation
6
Damage dose (Kt) was estimated to compare microstructure parameters of the test specimens cut out from the fuel claddings and guide tubes. The following work was done for this purpose:
Gamma emission spectrum recording that was followed by the analysis of 94Nb lines.
Calculation of specific activity (А).
Neutronic calculations of damage dose with the use of code UPM_PREPRO-2017_FENDL-2.0_ENDF/B-VII.0_Spectr based on a priori neutron spectrum for the VVER-1000 core.
Chart: Damage dose, dpa
| 15.4 | 17.100000000000001 | 16.2 | 6.8 | 10.9 | 10.6 | 10.6 | 14.6 | 14.4 | 14.3 | 17.600000000000001 | 4.0999999999999996
 | 1307.4572 | 1450.2583 | 1376.0944 | 615.3615 | 983.5047 | 956.6554 | 958.371 | 1239.5455 | 1261.0133 | 1251.6518 | 1496.6519 | 384.3893
Кt = A/86.485
There were only the 94Nb line in the built-up gamma spectrum that is why reconstruction of neutron spectrum did not allow for affecting its shape so the reference spectrum was taken (the neutron spectrum was normalized as to the reactor power level).

## Slide 7: β-Nb phase in alloy E110 before irradiation
7
It is a basic phase in the binary alloys Zr-Nb (E110, E125), it has BCC-crystalline lattice with a parameter а=0.331 nm.
Dav, µm | ρ, 1019 m-3 | V fraction, %
~ 45 | ~ 20 | 1.7
Chart: Diameter, nm
| 74 | 39 | 55 | 28 | 61 | 96 | 91 | 70 | 19 | 113 | 27 | 23 | 162 | 32 | 30 | 33 | 25 | 106 | 59 | 29 | 53 | 78 | 102 | 23
Zr | 11.3 | 13.1 | 13.4 | 15.2 | 12.4 | 10.9 | 12.3 | 10.6 | 18.1 | 11.7 | 18.4 | 15.2 | 11.8 | 16.1 | 15.5 | 13.2 | 12.5 | 11 | 10.4 | 13.2 | 11 | 10.2 | 9.4 | 12.4
Nb | 88.7 | 86.9 | 86.6 | 84.8 | 87.6 | 89.1 | 87.7 | 89.4 | 81.9 | 88.3 | 81.6 | 84.8 | 88.2 | 83.9 | 84.5 | 86.8 | 87.5 | 89 | 89.6 | 86.8 | 89 | 89.8 | 90.6 | 87.6
Nb 85 – 90 at.%
(extraction replica)

## Slide 8: Changes in the elemental composition of the β-Nb phase under irradiation
8
The composition of the β-Nb phase particles depends on their size and damage dose:
the smaller diameter the less is the percentage composition of Nb;
The higher the damage dose the less is Nb content.
Chart: 2 dpa
| 95 | 41 | 20 | 23 | 92 | 125 | 101 | 47 | 68 | 59 | 83 | 66 | 27 | 120 | 105 | 39 | 111 | 98 | 129 | 22 | 41
Zr | 9.31 | 12.27 | 14.51 | 14.3 | 10.68 | 8.9 | 10.61 | 11.63 | 12.11 | 11.33 | 9.53 | 11.13 | 13.27 | 10.59 | 9.81 | 11.66 | 10.42 | 9.58 | 10.91 | 13.8 | 10.96
Nb | 90.69 | 87.73 | 85.49 | 85.7 | 89.32 | 91 | 89.39 | 88.37 | 87.89 | 88.67 | 90.47 | 88.87 | 86.73 | 89.41 | 90.19 | 88.34 | 89.58 | 90.42 | 89.09 | 86.2 | 89.04
Chart: 7 dpa
| 95 | 128 | 93 | 70 | 86 | 90 | 150 | 62 | 52 | 88 | 46 | 68 | 121 | 103 | 72 | 77 | 102 | 47 | 45 | 142 | 145 | 117 | 127 | 31 | 62 | 43 | 160 | 153
Zr | 28.87 | 23.3 | 29.64 | 29.53 | 25.84 | 25.44 | 22.95 | 32.14 | 38.47 | 26.79 | 35.21 | 31.67 | 18.87 | 21.56 | 28 | 22.41 | 21.66 | 33.87 | 34.87 | 23.52 | 17.91 | 22.62 | 22.2 | 45.86 | 35.35 | 40.46 | 18.99 | 20.51
Nb | 71.13 | 75.7 | 70.36 | 70.47 | 74.16 | 74.56 | 77.05 | 67.86 | 61.53 | 73.21 | 64.79 | 68.33 | 81.13 | 78.44 | 72 | 77.59 | 78.34 | 66.13 | 65.13 | 76.48 | 82.09 | 77.38 | 77.8 | 54.14 | 64.65 | 59.54 | 81.01 | 79.49
Chart: 11 dpa
| 91 | 69 | 39 | 49 | 111 | 43 | 159 | 76 | 114 | 66 | 51 | 30 | 56 | 42 | 89 | 134
Zr | 33.86 | 43.79 | 49 | 42.61 | 30.37 | 48.82 | 26.94 | 36.31 | 29.7 | 42.59 | 44.27 | 48.22 | 42.94 | 53.24 | 34.38 | 28.51
Nb | 66.14 | 56.21 | 51 | 57.39 | 69.63 | 51.18 | 73.06 | 63.69 | 70.3 | 57.41 | 55.73 | 51.78 | 57.06 | 46.76 | 65.62 | 71.49
Chart: 17 dpa
| 81 | 77 | 116 | 111 | 57 | 82 | 44 | 134 | 83 | 56 | 122 | 61 | 56 | 48 | 34 | 154 | 110 | 97 | 96 | 93
Zr | 41.8 | 40.94 | 34.28 | 35 | 44.41 | 38.01 | 49.85 | 35.15 | 38.35 | 45.06 | 35.78 | 44.48 | 48.68 | 45.25 | 50.47 | 32.26 | 36.47 | 36.23 | 37.6 | 38.16
Nb | 58.2 | 59.06 | 65.72 | 65 | 55.59 | 61.99 | 50.35 | 64.85 | 62.65 | 54.94 | 64.22 | 55.52 | 51.32 | 54.75 | 49.53 | 67.74 | 63.59 | 63.77 | 62.4 | 61.84

## Slide 9: Changes in the elemental composition of the β-Nb phase under irradiation
9
Nb content in the particles of the β-Nb phase with a diameter of 50 nm and 150 nm in relation to the attained damage dose at an irradiation temperature of 330оС
Chart: Damage dose, dpa
| 0 | 11.4 | 10.7 | 11.1 | 16.8 | 7.1 | 14.3 | 16.2 | 16.3 | 16.100000000000001 | 17.3 | 19 | 4.4000000000000004
50 нм | 90 | 50 | 57 | 53 | 50 | 62 | 50 | 50 | 50 | 50 | 49 | 48 | 77
150 нм | 90 | 72 | 71 | 71 | 67 | 78 | 62 | 68 | 64 | 63 | 67 | 60 | 86
Damage dose | Dav, nm | ρ, 1019 m-3 | V fraction, %
0 dpa | ~ 45 | ~ 20 | 1.7
15 dpa | ~ 52 | ~ 12 | 1.2
Ingress of Zr from the matrix to the β-Nb phase leads to changes in size, concentration, and volume concentration of phase particles. BCC-lattice is preserved.
Nb content in the irradiated particles of the β-Nb phase in relation to the irradiation temperature
Chart: 13 dpa
| 104 | 71 | 70 | 111 | 56 | 43 | 117 | 76 | 79 | 122 | 92 | 121 | 83 | 59 | 82 | 48 | 84 | 103 | 70 | 58 | 50 | 61 | 92 | 54
360°С | 64.21 | 57.55 | 56.36 | 63.02 | 52.49 | 49.4 | 64.91 | 58.67 | 59.74 | 64.18 | 63.9 | 65.22 | 60.25 | 53.92 | 61.04 | 48.85 | 59.54 | 62 | 58.15 | 54.87 | 47.75 | 54.78 | 61.89 | 51.73
320°С | 53.2 | 52.44 | 53.87 | 58.31 | 53.78 | 60.85 | 60.91 | 42.9 | 57.53 | 52.29 | 48.44 | 53.8 | 54.65 | 58.38 | 55.15 | 57.61 | 56.1 | 43.41 | 50.06 | 47.46 | 49.19 | 58.84 | 59.39 | 59.75 | 64.95 | 50.1 | 43.46 | 51.16 | 42.91 | 58.03 | 54.26 | 55.23 | 55.44 | 59.55 | 60.49 | 63.25 | 55.18 | 56.28

## Slide 10: Laves phase Zr(Nb,Fe)2 in alloy E635 before irradiation
10
HCP а=5.3 Å, с=8.7 Å
Chart: Equivalent diameter, nm
| 33 | 47 | 48 | 50 | 52 | 53 | 56 | 57 | 62 | 72 | 73 | 75 | 76 | 83 | 95 | 95 | 97 | 102 | 104 | 111 | 118 | 119 | 122 | 128 | 140 | 141 | 160 | 165 | 166 | 177 | 185 | 188 | 188 | 190 | 194 | 198 | 198 | 204 | 212 | 213 | 214 | 217 | 220 | 230 | 230 | 240 | 244 | 252 | 252 | 258 | 268 | 280 | 283 | 306 | 307 | 323 | 335 | 344 | 446
Zr | 37.9 | 35.7 | 36.7 | 35.5 | 35.5 | 35.2 | 36.2 | 36 | 35.3 | 34.8 | 36.2 | 35.4 | 36.6 | 35.3 | 35.9 | 35.7 | 34.4 | 35.3 | 35.3 | 35.1 | 36.8 | 35.5 | 34.5 | 34.1 | 36.2 | 34.9 | 35.1 | 34.4 | 35.9 | 34.8 | 34.6 | 35.4 | 35 | 35.6 | 34.1 | 35.7 | 35.1 | 34.8 | 35.2 | 36.4 | 36.1 | 34.8 | 33.5 | 34.5 | 34 | 34.3 | 33.4 | 34.5 | 34.2 | 35.4 | 34.1 | 34.2 | 34.4 | 34 | 34 | 35.2 | 34.1 | 34.4 | 34.7
Nb | 33.3 | 35.3 | 34.1 | 34.5 | 33.9 | 34.2 | 35 | 33.9 | 32.3 | 32.8 | 34.4 | 33.7 | 33.2 | 33.4 | 34.5 | 32.9 | 32.6 | 32.9 | 33.9 | 33.6 | 32.7 | 34.5 | 33.2 | 32.6 | 31.3 | 32.2 | 32.4 | 31.1 | 33 | 31.9 | 31.3 | 30.4 | 30.5 | 31.5 | 31.9 | 30.2 | 32.4 | 31.4 | 31.4 | 30.7 | 31.2 | 33 | 31.3 | 31.5 | 31.2 | 30.8 | 32 | 31.1 | 33 | 31.8 | 33.3 | 31.7 | 32.1 | 32.4 | 31.1 | 30.9 | 32.5 | 31.6 | 31.9
Fe | 28.8 | 29 | 29.2 | 30 | 30.7 | 30.5 | 28.8 | 30.1 | 32.4 | 32.5 | 29.4 | 30.9 | 30.2 | 31.3 | 29.6 | 31.4 | 32.9 | 31.8 | 30.8 | 31.3 | 30.5 | 29.9 | 32.3 | 33.3 | 32.5 | 33 | 32.5 | 34.5 | 31.1 | 33.3 | 34 | 34.3 | 34.4 | 32.8 | 34 | 34.1 | 32.5 | 33.9 | 33.4 | 32.9 | 32.7 | 32.2 | 35.2 | 33.9 | 34.8 | 34.9 | 34.5 | 34.4 | 32.8 | 32.8 | 32.6 | 34.1 | 33.5 | 33.6 | 34.9 | 33.9 | 33.4 | 33.9 | 33.3

## Slide 11: Changes in the elemental composition of the Laves phase Zr(Nb,Fe)2 under irradiation
11
Under neutron irradiation Fe atoms leaves the Laves phase particles Zr(Nb,Fe)2 and enters the matrix and thus the elemental composition of particles and matrix changes.
Chart: 2.5 dpa
| 257 | 64 | 38 | 169 | 308 | 202 | 169 | 224 | 38 | 174 | 186 | 131 | 184 | 56 | 115 | 243 | 297 | 175 | 151 | 158 | 141 | 168 | 85 | 103 | 50 | 65 | 272 | 36 | 309
Zr | 39.28 | 38.24 | 34.91 | 37.75 | 38.64 | 38.8 | 40.25 | 39.07 | 34.92 | 38.14 | 38.26 | 39.41 | 40.58 | 41.05 | 39.58 | 39.1 | 38.51 | 39.2 | 42.19 | 38.75 | 40.79 | 40.35 | 40.34 | 41.17 | 36.83 | 38.5 | 38.49 | 40.01 | 38.49
Nb | 37.82 | 43.77 | 49.59 | 38.91 | 35.29 | 40.58 | 43.15 | 35.06 | 50.61 | 39.2 | 40.51 | 42.33 | 42.39 | 43.57 | 43.72 | 37.28 | 39.3 | 41.56 | 45.96 | 40.21 | 42.59 | 44.11 | 47.03 | 47.01 | 50.96 | 40.79 | 39.53 | 51.22 | 37.04
Fe | 22.9 | 17.99 | 15.5 | 23.34 | 26.07 | 20.35 | 16.6 | 25.87 | 14.47 | 22.66 | 21.22 | 18.27 | 17.02 | 15.38 | 16.71 | 23.62 | 22.19 | 19.24 | 11.84 | 21.03 | 16.62 | 15.53 | 12.63 | 11.82 | 12.21 | 20.7 | 21.98 | 8.77 | 24.48
Chart: 11 dpa
| 195 | 125 | 233 | 215 | 207 | 86 | 33 | 42 | 75 | 85 | 192 | 269 | 120 | 126 | 335 | 72 | 158 | 197 | 152 | 168 | 98 | 293 | 272 | 350
Zr | 47.7 | 47.87 | 46.96 | 46.71 | 46.13 | 51.47 | 51.61 | 53.9 | 52.92 | 53.93 | 45.93 | 46.44 | 54.61 | 49.44 | 46.79 | 52.38 | 48.7 | 47.55 | 49.99 | 48.95 | 50.41 | 46.66 | 47.68 | 46.48
Nb | 46.64 | 47.74 | 49.04 | 47.73 | 47.23 | 46.92 | 47.73 | 45.63 | 46.01 | 45.61 | 48.36 | 45.9 | 44.74 | 48.47 | 47.83 | 47.26 | 48.25 | 47.85 | 47.65 | 47.67 | 48.88 | 47.63 | 47.76 | 48.46
Fe | 5.66 | 4.39 | 4 | 5.56 | 6.64 | 1.61 | 0.66 | 0.46 | 1.08 | 0.46 | 5.71 | 7.66 | 0.65 | 2.09 | 5.38 | 0.36 | 3.04 | 4.6 | 2.36 | 3.38 | 0.71 | 5.71 | 4.56 | 5.06
Chart: 16 dpa
| 168 | 330 | 221 | 250 | 295 | 201 | 144 | 82 | 51 | 102 | 221 | 137 | 64 | 222 | 38 | 56 | 38 | 98 | 68 | 123 | 257 | 37
Zr | 52.3 | 51.6 | 53.8 | 53.8 | 53.7 | 53.1 | 53.5 | 53.9 | 53.3 | 54.3 | 53 | 50.9 | 50.7 | 52.3 | 49.7 | 50.9 | 53.1 | 52.1 | 52.4 | 52.6 | 53.8 | 52.7
Nb | 46.7 | 46.8 | 45.6 | 45.5 | 45.3 | 46 | 46.5 | 46.1 | 46.7 | 45.7 | 46.3 | 48.1 | 49.3 | 46.9 | 50.3 | 49.1 | 46.9 | 47.9 | 47.6 | 46.7 | 45.3 | 47.3
Fe | 0.9 | 1.6 | 0.7 | 0.7 | 1 | 1 | 0 | 0 | 0 | 0.87 | 0.7 | 1 | 0 | 0.8 | 0 | 0 | 0 | 0 | 0 | 0.7 | 0.8 | 0
Specimens were cut out from the guide tube (Тirr=310 оС)
Chart: Damage dose, dpa
| 0 | 2.2667221112852061 | 10.380059236711579 | 15.442881800726628 | 13.28870547667278 | 2.5259490620522755 | 7.4052257448382379 | 10.482617796337818 | 9.2693335151877587 | 6.3 | 9.3000000000000007 | 7
250 nm | 33 | 23 | 5 | 1.5 | 0.7 | 20 | 8 | 4 | 5.5 | 8 | 6 | 8.5
50 nm | 30 | 15 | 0.5 | 0.5 | 0.5 | 8 | 2 | 0.5 | 1 | 2.5 | 1

## Slide 12: Changes in the elemental composition of the Laves phase Zr(Nb,Fe)2 under irradiation
12
Fe leaves the particles of the Laves phase Zr(Nb,Fe)2 and enters the matrix beginning with the periphery
Damage dose
2.5 dpa
Тirr=310оС
Damage dose
13 dpa
Тirr=310оС

## Slide 13: Transformation of Laves phase Zr(Nb,Fe)2 under irradiation
13
Single-crystal Laves phase transforms into polycrystalline phase β-Nb in stages
Stage I
Unirradiated
Stage II
Stage III
Stage IV
HCP
BCC
β-Nb

## Slide 14: Transformation of Laves phase Zr(Nb,Fe)2 under irradiation
14
Schematic representation of the stage-by-stage transformation
HCP
BCC

## Slide 15: Radiation-induced finely dispersed phase
15
Finely dispersed laminary phase forms under irradiation in E110 and E635 alloys.
Particles of radiation-induced finely dispersed phase in alloy E110 after neutron irradiation up to a damage dose of 12 dpa (a, b) and 9 dpa (c).
a
b
c

## Slide 16: Radiation-induced finely dispersed phase
16
Finely dispersed phase is larger in alloy E110 and its concentration is 7 times higher compared to alloy Э635.
Chart: Damage dose, dpa
| 10.1 | 10.1 | 7 | 11.1 | 10.7 | 14.3 | 2 | 12.7 | 14.472472534841907 | 16.100000000000001 | 17.3 | 12.8 | 1.1769999999999998 | 2.7 | 14.7 | 1.1964808348830103 | 1.6 | 14.580716773925182
ВВЭР-1000 | 20 | 17.3 | 12.2 | 21 | 18.2 | 20 | 5 | 18 | 9.7 | 18 | 14 | 15 | 21 | 13 | 12.1 | 12 | 31 | 10 | 14 | 14
Chart: Damage dose, dpa
| 13.5 | 15.4 | 16.2 | 11 | 6.3 | 14.3 | 10.199999999999999 | 10.7 | 7.3
ВВЭР-1000 | 2.5 | 2.4 | 2.8 | 2.1 | 0.2 | 3 | 0.7 | 1.3 | 0.8
Chart: Damage dose, dpa
| 10.4 | 13.5 | 15.4 | 16.2 | 11 | 6.3 | 14.3 | 10.199999999999999 | 10.7 | 7.3
ВВЭР-1000 | 2.8 | 2.9 | 3.4 | 4 | 2.9 | 2.5 | 3.7 | 4.4 | 3.6 | 3.1
Alloy E635
Alloy E110
Chart: Damage dose, dpa
| 10.1 | 10.1 | 7 | 11.1 | 10.7 | 14.3 | 2 | 12.7 | 14.472472534841907 | 16.100000000000001 | 17.3 | 12.8 | 1.1769999999999998 | 2.7 | 14.7 | 1.1964808348830103 | 1.6
ВВЭР-1000 | 5.65 | 5.22 | 4.6 | 5.45 | 5.8 | 6.03 | 3 | 6.7 | 3.5333 | 5.85 | 2.02 | 6 | 6.6433 | 5.9 | 2.6 | 3.38 | 6.25 | 3.2 | 2.58
2,5∙1021 m-3
17∙1021 m-3
~ 6 nm
~ 3 nm

## Slide 17: Conclusions
17
β-Nb
Nb content in the particles depends on their size and irradiation temperature: the smaller the particle and lower the irradiation temperature, the lower is percentage composition of Nb. The higher is the damage dose, the percentage composition of Nb becomes lower in the particles, their size increases, concentration decreases but the BCC-structure is preserved.
Laves phase Zr(Nb,Fe)2
If damage dose is lower than 15 dpa, Fe content in the particles depends on their size (the smaller the particle, less Fe it contains). Further irradiation leads to Fe escapes from the phase and enters the matrix , and thus the crystalline lattice transforms from HCP into BCC in stages. Transformation begins with the periphery and propagates towards the center of particles. As a result, initial single-crystal Laves phase becomes polycrystalline composed of the β-Nb grains. Further irradiation does not change the composition of new polycrystalline phase and its size.
Radiation-induced phase
Neutron irradiation in a temperature range of 290ºC to 340оС leads to formation of radiation-induced finely dispersed laminary phase β-Nb of size no more than 10 nm in alloys E110 and E635. Its concentration attains the saturation (17·1021m-3 for E110 ) once the damage dose higher than 10 dpa has been attained. Concentration of phase particles is 7 times higher in alloy E110 compared to alloy Э635.
Neutron irradiation in a temperature range of 290ºC to 340оС results in significant changes in parameters of the secondary phases.

## Slide 18: THANK YOU FOR YOUR ATTENTION!
A.V. Obukhov, Senior Researcher
Tel: 8(84235)94947
E-mail: gpk@niiar.ru